## Slide 1: A fully coupled implementation of hydrogen embrittlement in FE analysis
Daniel Huang
Department of Mechanical Engineering
Aalto University

## Slide 2
The paper provides a guideline and codes through a practical case:
A cohesive zone model simulates the fracture toughness test of a C(T) specimen charged with hydrogen. The model in the fully coupled formulation is enriched with a sensitivity analysis to prove the capability under different conditions.
Target: Fully coupled vs Weakly coupled & Theoretical Explanation

## Slide 3: Contnets
Background
Scope
Theoretical Explanation
Assumptions
Comparison
Conclusion

## Slide 4
Hydrogen Embrittlement Theories
Hydrogen reaction embrittlement
Internal reversible hydrogen embrittlement
Hydrogen environmental embrittlement
Hydrogen Embrittlement Mechanics
Hydrogen-Enhanced Localized Plasticity (HELP)
Hydrogen-Enhanced Decohesion (HEDE)
Hydrogen-Induced Phase Transformations
Hydrogen-Enhanced Strain-Induced Vacancies
Hydrogen Trapping
Hydrogen-vacancy interactions
Adsorption-Induced Dislocation Emission
Hydride formation
Different Approach
Atomistic simulation (Analysis Method)
Influence of Stacking Fault Energy
Peridynamic Hydrogen Embrittlement Model (Analysis Method)
Local Stress Criterion
Phase Field-Based Models (Analysis Method)
Combined Effect of Hydrogen Embrittlement and Loss of Constraint
THEORETICAL BACKGROUND

## Slide 5
BACKGROUND CONDITION
AISI 4130 steel
A HEDE mechanism is simulated scaling the TSL
Heat transfer replace mass diffusion
Macro level discussion
Replace Fourier law with user defined function

## Slide 6
SCOPE
Static Analysis
Diffusion Analysis
Static Analysis
Weakly Coupled
Fully Coupled
UMATHT
Material property and stress
Crack Propagation
Hydrogen diffusion
FEM Mesh

## Slide 7
THEORETICAL EXPLANATION
BASIC RELATION
Continuity Equation (Hydrogen Diffusion)
H number unit V
H flux
Continuity Equation (Heat Transfer)
Internal thermal energy per unit mass
Density
Heat Flux
Heat Source

## Slide 8
THEORETICAL EXPLANATION
CONCENTRATION AND FLUX
Diffusible H
Trapped H
H concentration
Flux With
Diffusible H
Effective Diffusivity
Diffusible H Gradient
Internal condition
Universal Gas Constant & Temperature
Hydrostatic Stress Gradient
(- + )
Ideal Gas Law
Mole number
Partial Molar Volume
External condition
Gradient of Diffusible H
Gradient of Hydrostatic
Fick’s First Law
Hydrogen Flux
Flux

## Slide 9
THEORETICAL EXPLANATION
TRAPPED CONCENTRATION
Oriani’s theory for trapped H
Continuity Equation (Hydrogen Diffusion)
H concentration
Hydrogen Flux
Diffusible H
Interstitial lattice sites density
Trapped H
Trap site density
Equilibrium constant
Arrhenius Equation
Binding enthalpy ΔWB=-60kJ/mol

## Slide 10
THEORETICAL EXPLANATION
CONCENTRATION SITE DENSITIES
Oriani’s theory for trapped H
Interstitial density for α-Fe
Avogadro Constant=
6.02214076×10 ^23 /mole
Number of interstitial =6
Iron Density=7.87×103 kg/m3 at 293 K
Molar mass = 55.8×10-3 kg/mol3 at 293 K
Trap site density
Experimental (Kumnick and Johnson)
Plastic strain
Sofronis method
Lattice parameter= 2.86 × 10^10m (BCC iron)
Dislocation density
1 × 10^10 m/m^3 (Annealed)
1 × 10 ^16 m/m^3 (Max)
2 × 10^16m/m^3
Notes:
Sofronis method compared McNabb-Foster (CT not direct to CL) and Oriani's theories

## Slide 11
THEORETICAL EXPLANATION
FLUX HYDROSTATIC STRESS
Hydrostatic Stress Gradient
Element and nodal shape functions
Hydrostatic stress relates to coordinate
Averaging extrapolated nodal stress
Stress field from interpolated nodal stresses and shape function
Coordinate Conversion
Jacobian Matrix

## Slide 12
THEORETICAL EXPLANATION
FINAL VARIABLE
The basic Abaqus thermal model refers to the Fourier law, which can’t implement the complex relations defined earlier. Therefore, UMATHT subroutine was used.

## Slide 13
THEORETICAL EXPLANATION
CONCENTRATION INCREMENT
Chain rule with partial derivatives
Experimental (Kumnick and Johnson)
Sofronis method
H concentration
H concentration increment (Fully coupled)
Concentration at time t
Concentration difference according to diffusible H
Concentration difference according to trapped H (Plastic Strain)

## Slide 14
THEORETICAL EXPLANATION
PARAMETERS AND CONNECTIONS
identity tensor

## Slide 15
THEORETICAL EXPLANATION
TSL AND CONCENTRATION
Variation of Gibbs free energy=30kJ/mol
Hydrogen concentration
Hydrogen coverage factor
Limit stress of the cohesive element (Pa)
Factor decreasing cohesive strength (HEDE mechanism)
Traction Separation Law
(Selected trapezoidal shape with four parameters)

## Slide 16
ASSUMPTION AND SELECTIONS
Density (Continuity equation) equals to 1
Binding Enthalpy (Activation energy) equals to -60kJ/mole and A=1(Arrhenius equation )
Sofronis Method Assumptions
Extrapolation data for the hydrostatic stress calculation
Initial concentration is 1.5 ppm and uniformly distributed on the samples
Interstitial Density values
TSL shape and parameter selection
Gibs free energy as 30kJ/mol

## Slide 17
FEM SETTING
Symmetric model
Linear quadrilateral elements with plane strain formulation
Mesh is progressively refined, up to 15.6 μm to the symmetric plane
Mesh of cohesive elements with rectangular shape (0.53 mm high and 1.53 mm long, ahead of the crack tip) are approach around crack tips
TSL parameters with Relaxed ratios between the separations δi for calibration

## Slide 18
COMPARISON
Hydrostatic stress
gradient
Hydrostatic stress

## Slide 19
SENSITIVITY
Selection of DL and C0 according to the case condition
C0 between 0.5 and 3 ppm
DL between 1*10^-3 to 1*10^-6 mm^2/s

## Slide 20
CONCLUSION
Possible of many mechanism acting at the same time but not only HEDE
Subroutine UMATHT is called when the time increment is not yet converged, so that actually the present implementation uses Δεp estimated at the preceding converged increment. However, for small Δt the associated error is considered negligible.

## Slide 21
NEXT STEP
Primary:
  Compare and analysis more closely our fully coupled model with presented one
Secondary:
  More learning on Abaqus
Ultimate Goal
  Improving the model and apply in Abaqus or Mathematica

## Slide 22
Thank you!